## Slide 1: McStas samples for diffraction
Erik Knudsen

## Slide 2
General concepts (reminder)
Focus on diffraction-oriented samples:
    Incoherent scatterer
    Powder
    Single Crystal
    File formats
Agenda

## Slide 3: Add a slide on elastic scattering…

## Slide 4
Incoherent.comp
An incoherent scatterer with various sample shape options
Samples - Incoherent
Incoherent Sample

## Slide 5
Incoherent.comp
An incoherent scatterer with various sample shape options
Incoherent Sample
        p_interact = The probability that a given ray will interact (scatter) with a sample. Does not directly affect the intensity – only the quality of the resulting Monte Carlo estimate.

## Slide 6
Crystalline Samples

## Slide 7
From single crystal / crystallites to powder….
Single crystal
Polycrystal with a little disorder, i.e. a preferred orientation, texture
Powder with complete disorder

## Slide 8
Single Crystal model
Courtesy University College London
Models ideally imperfect crystal:
  Peak broadening is dominated by mosaic => not appropriate for highly perfect crystals.
  “Space group symmetries” considered out of scope.
  Optimized for small unit cells but…
  No assumption about unit cell, orientation etc.
  Gaussian model for mosaic (see later)

## Slide 9
Single Crystal

## Slide 10
Single Crystal
Unit cell vectors (ax,ay,az, bx, by,bz, cx,cy, cz). Encodes the crystal orientation relative to the Component’s orientation

## Slide 11
Single Crystal
Mosaicity parameters: mosaic, mosaic_a, mosaic_b, mosaic_c, mosaic_AB

## Slide 12
Single Crystal mosaicity

## Slide 13
Single Crystal mosaicity
Three models:
Isotropic Mosaicity = Gaussian distribution of rotation angle, with given standard deviation, around a random vector.
Anistropic mosaicity = Gaussian distribution of angles around each of the unit cell axis.

## Slide 14
Single crystal mosaicity
Three models:
Isotropic Mosaicity = Gaussian distribution of rotation angle, with given standard deviation, around a random vector.
Anistropic mosaicity = Gaussian distribution of angles around each of the unit cell axis.
“Rocking curve mosaic” = Gaussian distr. around axis determined by width of two given Bragg peaks. Specify &sigma, and hkl for two peaks.

## Slide 15
9.2 PowderN

## Slide 16
PowderN inputs

## Slide 17
PowderN inputs
Sampling parameters
Concentric = Hollow Powder [cylinder]

## Slide 18
PowderN inputs
Sampling parameters
Concentric = Hollow Powder [cylinder]
Sampling parameters

## Slide 19
Sampling parameters
PowderN inputs
Concentric = Hollow Powder [cylinder]
0
1
2
2
3
3
4
5
A
B
C

## Slide 20
PowderN concentric in code
COMPONENT Al = PowderN(
reflections="Al.laz", radius=0.02, yheight=0.05, thickness=0.005,
p_transmit=0.8, concentric=1)
AT (0, 0, 0) RELATIVE PREVIOUS
COMPONENT al2co3 = PowderN(
reflections=Al2CO3-laz, radius=0.005, yheight=0.05,
p_inc=0.15, p_transmit=0.5)
AT (0, 0, 0) RELATIVE PREVIOUS
COMPONENT Al_2 = COPY(Al)(concentric=0)
AT (0,0,0) RELATIVE PREVIOUS
Sampling parameters
0
1
2
2
3
3
4
5
A
B
C

## Slide 21
PowderN inputs
Only scatter into a part of 4π

## Slide 22
PowderN inputs
Only scatter into a part of 4\pi

## Slide 23
PowderN inputs
Only scatter into a part of 4\pi
d_phi

## Slide 24
Reflection files for Single_crystal and PowderN
# TITLE *Aluminum-Al-[FM3-M] Miller, H.P.jr.;DuMond, J.W.M.[1942] at 298 K
# CELL 4.049320 4.049320 4.049320 90.000000 90.000000 90.000000
# SPCGRP F M 3 M CUBIC STRUCTURE
# ATOM AL 1 0.000000 0.000000 0.000000
# SCATTERING FACTOR COEFFICIENTS: AL F= 0.345 CM-12
# Reference: Physical Review (1940) 57, 198-206
#
# Physical parameters:
# sigma_coh 1.495 coherent scattering cross section (single atom) in [barn]
# sigma_inc 0.0082 incoherent scattering cross section (single atom)in [barn]
# sigma_abs 0.231 absorption scattering cross section (single atom) in [barn]
# density 2.70 in [g/cm^3]
# weight 26.98 in [g/mol] (single atom)
# multiplicity 4 in [atoms/unit cell]
# Vc 66.4 volume of unit cell in [A^3]
# v_sound 5100 in [m/s]
# v_sound_l 6420 velocity of longitudinal sound in [m/s]
# v_sound_t 3040 velocity of transversal sound in [m/s]
# T_m 933.5 melting temperature in [K]
# T_b 2792.2 boiling temperature in [K]
# At_number 13 atomic number Z
# lattice_a 4.04932 lattice parameter a in [Angs]
#
# Format parameters: Crystallographica format
# column_j 4 multiplicity 'j'
# column_d 5 d-spacing 'd' in [Angs]
# column_F2 7 norm of scattering factor |F|^2 in [fm^2]
# column_h 1
# column_k 2
# column_l 3
#
# h k l Mult. d-space 2Theta F-squared
-1 -1 -1 8 2.338 24.6973 21.3
-1 -1 1 8 2.338 24.6973 21.3
…
Lau datafiles
header
+
reflection list
Can be used with Single_crystal, PowderN, Isotropic_Sqw

## Slide 25
Input for the PowderN
# TITLE *Corundum-Al2O3-[R3-CH] Graafsma, H.;Souhassou, M.;Harkem[1998] [corundum saphire:blue, ruby:red]
# CELL 4.757000 4.757000 12.987700 90.000000 90.000000 120.000000
# SPCGRP R -3 C TRIGONAL STRUCTURE
# ATOM AL 1 0.000000 0.000000 0.352110
# ATOM O 1 0.306260 0.306260 0.250000
# SCATTERING FACTOR COEFFICIENTS: AL F= 0.345 CM-12 ; O F= 0.581 CM-12
# Reference: Acta Crystallographica B (1998) 54, 193-195
#
# Physical parameters:
# sigma_coh 15.683 coherent scattering cross section for Al2O3 in [barn]
# sigma_inc 0.0188 incoherent scattering cross section for Al2O3 in [barn]
# sigma_abs 0.4625 absorption scattering cross section for Al2O3 in [barn]
# density 4.05 in [g/cm^3]
# weight 101.96 in [g/mol] for Al2O3
# multiplicity 6 in [Al2O3/unit cell]
# Vc 254.52 volume of unit cell in [A^3]
# T_m 2273 melting temperature in [K]
# T_b 3773 boiling temperature in [K]
# lattice_a 4.757 lattice parameter a in [Angs]
# lattice_c 12.9877 lattice parameter c in [Angs]
# lattice_cc 120 lattice angle gamma in [deg]
#
# Format parameters: Lazy format <http://icsd.ill.fr>
# column_j 17 multiplicity 'j'
# column_d 6 d-spacing 'd' in [Angs]
# column_F 13 norm of scattering factor |F| in [barn]
# column_h 1
# column_k 2
# column_l 3
#
# H K L THETA 2THETA D VALUE 1/D**2 SIN2*1000 H K L INTENSITY /F(HKL)/ A(HKL) B(HKL) PHA.ANG. MULT LPG
1 0 1 6.35 12.71 4.5175 0.0490 12.25 1 0 1 367.0 4.1 -4.08 0.00 180.00 6 82.14
0 0 3 7.10 14.20 4.0467 0.0611 15.27 0 0 3 110.0 4.3 4.32 0.00 0.00 2 66.01
0 1 2 7.57 15.13 3.7972 0.0694 17.34 0 1 2 10.9 0.8 0.84 0.00 0.00 6 58.18
…
Laz + Lau datafiles
header
+
reflection list
Can be used with PowderN, Isotropic_Sqw

## Slide 26
What’s already there?
Single Crystals
Powders
Ag.laz
Al.laz
Al2O3_sapphire.laz
Au.laz
B4C.laz
Ba.laz
Be.laz
BeO.laz
Bi.laz
C_diamond.laz
C_graphite.laz
Cd.laz
Cr.laz
Cs.laz
Cu.laz
Cu2MnAl.laz
Fe.laz
Fe_Gamma.laz
Ga.laz
Gd.laz
Ge.laz
H2O_ice_1h.laz
He4_hcp.laz
Hg.laz
I2.laz
K.laz
Li.laz
LiF.laz
Mo.laz
Na2Ca3Al2F14.laz
Nb.laz
Ni.laz
Pb.laz
Pd.laz
Pt.laz
Rb.laz
Se_alpha.laz
Se_beta.laz
Si.laz
SiO2_quartza.laz
SiO2_quartzb.laz
Sn_alpha.laz
Sn_beta.laz
Ti.laz
Tl.laz
UO2.laz
V.laz
Y2O3.laz
Y3Fe5O12_YIG.laz
Zn.laz
Zr.laz
duplex.laz
Al.lau
Al2O3_sapphire.lau
B4C.lau
BCC_fake.lau
BeO.lau
C60.lau
C_diamond.lau
C_graphite.lau
CaF2.lau
Ge.lau
In.lau
PPase_D_P1.lau
Rubredoxin.lau
SiO2_cristobalite.lau
SiO2_quartza.lau
SiO2_quartzb.lau
TiO2_rutile.lau
YBaCuO.lau
adrenaline.lau
aspirin.lau
leucine.lau

## Slide 27
Where to get these files…
$MCSTAS/data
  Windows: c:\mcstas-2.5\lib\data
  Linux: /usr/(local)/share/mcstas/2.5/data
  OS X: /Applications/McStas-2.5/Contents/Resources/mcstas/2.5/data
- Or make your own via
  Finding a CIF file for the given structure
    e.g. from ICSD http://icsd.fiz-karlsruhe.de or COD <http://crystallography.net>
    Build one using VESTA
  Process it using
    cif2hkl which is available in your McStas installation

## Slide 28
McStas: structure: powder
For powders, the pure elastic diffraction is easy to prepare: LAZ
  PowderN
  Single_crystal(powder=1, ...)
  Isotropic_Sqw
Terminal:
cif2hkl --powder file.cif
CIF file
FullProf/ShelX
McStas Laz file

## Slide 29
McStas: structure: SX
For single crystals, the pure elastic diffraction is easy to prepare: LAU
  PowderN
  Single_crystal
  Isotropic_Sqw
Terminal:
cif2hkl --xtal file.cif
CIF file
FullProf/ShelX
McStas Lau file

## Slide 30
McStas uses a number of input data formats, all text based.
Lau (Single_crystal, PowderN, Isotropic_Sqw)
Laz (PowderN, Isotropic_Sqw)
Sqw (Isotropic_Sqw)
qSq (Isotropic_Sqw) – mostly for liquids
nxs (Sample_nxs) – this is not a NeXus/HDF
PDB (SANSPDB)
ncmat (NCrystal)
The question is how to generate these files…
By hand ?
McStas Data formats

## Slide 31
OFF/PLY any geometry
An additional complex geometry enables to use any point set to describe the material volume (geomview OFF file).