The “incoherent approximation”
The “phonon expansion”
Estimate S(q,w) from nearly nothing ?
E. Farhi, ILL.

---
Background – Old stuff !
- Most inelastic neutron scattering fundamental theory was written in the 50’-70’:
  → Sears, Sjölander, Egelstaff, van Hove, Squires, Oskotskii, Sköld, Carpenter, Schober ...
- Nothing really new since then.
- Remains in the text books, old software is deprecated. Not used much these days.
- Let’s recap these concepts...

---
The “generalised” density of states
- The generalised density of states (gDOS) formalism states that it is possible to write an “effective” density of states from a complex material made of d species with “partial” vDOS gd:
- It is often named “neutron weighted density of states”
- The gDOS (meas. average) is NOT the vDOS.
- Reminder: g(w) density of modes in [w,w+dw]
{%sigma} over {m} G( %omega) = sum_d {{%sigma_d} over { m_d} g_d( %omega )}

---
Density of states estimate
- Carpenter/Bellisent/Egelstaff:
  Cons: Measurement never reaches Q→0, and only use the smallest angle data (low statistics).
- Bredov/Oskotskii:
  Pros: Use the whole data set, integrated over the instrument dynamic range (higher statistics).
g( %omega) approx lim_{Q toward 0} {{ %omega } over { ( n(%omega)+1 ) Q^2} S_{inc}( Q,%omega )} approx lim_{Q toward 0} {{ %omega^2 } over { Q^2} S_{inc}( Q,%omega )}
g(%omega) approx {%omega int Q S(Q,%omega) e^{2W(Q)} dQ} over { [Q_{max}^4 - Q_{min}^4] [n(%omega)+1] }
iFit: ‘dos’ method for Sqw2D

---
The “incoherent approximation”
- The integrated ∫dQ or dq incoherent and coherent contributions are roughly equal (apart s).
- Consequence: the density of states g(w) can be obtained equally from coherent, incoherent and total scattering. Better use “Bredov”.
- Limitation: Exact for cubic monoatomic systems, can be extended to isotropic density materials (see gDOS).
- See: Oskotskii (1967)

---
Scattering law, harmonic
- The scattering law can be written:
  with partials:
- Writing R=R0+u, we can expand S.
s
autocorrelation of displacements
Small displ. (harmonic)
Equil.

---
Scattering law, harmonic
- Debye-Waller function
- Motion correlations:
  DON’T PANIC (yet)
Structure
Average
motions
Dynamics

---
Scattered intensity (interlude)
- Of course, the scattered intensity (differential cross section) is as usual:
- Monoatomic system: S(Q,w) = s Sk,k(Q,w)
- We usually only consider the 1st term in À.

---
S(Q,w) harmonic isotropic incoherent
- For a harmonic isotropic incoherent system:
- And:
- See: Sjölander (1958)
f(t)
Look at that one
Average
motions

---
The “phonon expansion”
- We develop the last exp[f(t)] term in Taylor series → “phonon expansion”
- The “phonon” terminology comes from the fact that initially, the partial SK,K’ includes both coherent and incoherent processes, and the high order terms correspond to multi-phonons.
- Phonons in an incoherent scatterer is somewhat odd.
T_1( %omega) = {g(%omega)} over { 2 hbar %omega } ( coth({hbar %omega} over {2 k T} ) + 1) newline T_p( %omega) = T_1( %omega) * T_{ p-1 }( %omega)
Tp obtained recursively

---
Let’s keep calm
- The p=0 term is the Elastic Incoherent Scattering Function (EISF) → DW.
- The p=1 term is the one-phonon (incoherent !) response:
- 2W(Q) = hQ2/2m ∫ T1(w) dw [often over estimated]
- For Q→0, Debye-Waller → 1. As n(w)+1 ~ 1/w we get an estimate of g(w) from S(Q,w):
T1(w)
lim_{ Q toward 0 } S( Q,%omega ) approx {Q^2} over {%omega^2} g( %omega)
[Bellissent-Funel 1991]

---
How to use this...
Input: s, m, g(w) , [optional: DW]
Output: Debye-Waller estimate 2W(Q), Sinc(Q,w)
Multi
Phonons
(inc)
s, m, g(w)
2W(Q), Sinc(Q,w)
iFit: ‘incoherent’ method for vDOS
Older code 1D: MUPHOCOR, LAMP

---
Does it work ?
- Monoatomic isotropic material: l-Al
- Can simulate liquid dynamics using DFT:
  - 200 atoms in a box, PAW PBE
  - 12000 MD steps of 3fs, T=1300 K → R(t)
  - Compute Sinc(q,w) Scoh(q,w) using MDANSE/nMoldyn
  - Compute the vDOS g(w) using MDANSE/nMoldyn
- Compute the incoherent from the vDOS and compare with the ‘true’ Sinc(q,w) from the MD.

---
Incoherent liq-Al: approximation
g(w)
l-Al
- R(t) → MDANSE → Sinc(Q,w)
- R(t) → MDANSE → g(w)
- iFit:
  - g=iData_vDOS(‘dos-lAl.nc’);
  - Sinc=plus(incoherent(g,'T',1300,'DW',0.01, ‘m’,27));
R(t) → MDANSE → Sinc
No DW factor, S(q)=1
g(w)→Sinc
Sinc(q) ➘
Not perfect, but ...

---
What about the coherent ?
- Al is a coherent scatterer
- Phenomenological guess [Sköld 1967]
S(Q)
L-Al
From MD
{S} rsub {coh} left (Q , ω right ) = S left (Q right ) {S} rsub {inc} left ({Q} over {sqrt {S left (Q right )}} , ω right )
Structure is ‘forced’ in.
Sköld
(coh)
Sinc(Q,w), S(Q)
Scoh(Q,w)
iFit: ‘coherent’ method for Sqw2D

---
Coherent liq-Al: approximation
- R(t) → MDANSE → Scoh(Q,w)
- R(t) → MDANSE → S(Q) or ∫Scoh(Q,w) dw
- iFit:
  - Sq=iData(‘Sq-lAl.nc’);
  - Scoh=coherent(Sinc, Sq);
S(Q)
l-Al
Sinc(Q,w), S(Q)→Scoh
R(t) → MDANSE → Scoh
No DW factor, S(q)=1
No phonons
(of course)
Not perfect, but ...

---
Partial summary
- If we have an estimate for the vDOS, we can compute the Sinc with a reasonable agreement.
  - This is the foundation for NJOY/LEAPR. g(w) can be estimated from neutron ToF experiment, MD and lattice dynamics (solids). Search literature !
- If in addition we have an estimate for the structure S(Q), we can also get Scoh.
WARNING: Not perfect, but we get it from very limited information.

---
More complex: water (liquid)
- GROMACS 4000 D2O, MD 2500 time steps
- R(t)→MDANSE→g(w)→Sinc
- Compare with Sinc from MD
- Get S(Q) from MD
- Estimate Scoh from [Sinc and S(Q)]
- WARNING: not exact: non monoatomic
g(w) from MD
l-D2O
293 K
S(Q) from MD
l-D2O
293 K

---
R(t) → MDANSE →Sinc (MD)
R(t) → MDANSE →Scoh (MD)
g(w)→Sinc (approx)
Sinc(Q,w), S(Q)→Scoh (approx)
Water (liquid)
D2O 293 K, S(Q,w)
Structure is there

---
Powders (solid, isotropic)
- VASP 200 Al atoms, PAW PBE. MD 300 K.
- Check for gDOS: coherent and incoherent estimates are equal (Bredov).
gDOS p-Al
iFit: g = dos(coh);
Sinc
MD p-Al, VASP
Scoh
S(Q) p-Al
iFit: sq = structure_factor(coh);

---
Sinc
MD p-Al, VASP
Scoh
Sinc
g(w) → approx
Scoh
Powder: p-Al
Well… that’s the same ?

---
Validity: Pros
- Pros:
  - Requires minimal info: g(w), S(q)
  - Very fast to compute.
  - Applicable to any isotropic material.
  - Not meant to be exact (strong hypothesis).
  - Acceptable results when nothing else exists: liquids, amorphous, powders, gases

---
Validity: Cons
- Cons:
  - Does not reconstruct low Q dynamics (phonons, …).
  - Structure is forced in, but does not satisfy De Gennes narrowing (narrow at Bragg peaks).
  - Incoherent estimate better than coherent one.
  - Would require partial g(w) and S(Q) per atom to improve accuracy.
  - Assumes cross terms SKK’ are null.

---
Applicability
- Experiments: total = coh+inc
- Can estimate incoherent quite well, to e.g. help subtract ‘background’ and better estimate the coherent part.
- Can build S(q,w) estimates from very little info.

---
Nuclear data bases
- Some of this is in NJOY/LEAPR module
  - Incoherent “phonon-expansion”
  - Coherent [Sköld] estimate only used for D2O
  - Contribution is in m-p / !p, usually p=5-10 is enough.
  - All materials, including coherent scatterers are assumed incoherent.
  - S(a=h2Q2/2mkT,b=-hw/kT) ~ S(Q,w)/Q depends on T, whereas S(Q,w) mostly changes around phase transitions (except for Bose factor).
  - Material descriptions in ENDF are few.

---
Nuclear data bases: D2O S(a,b)
- Get Bariloche “D in D2O” ENDF TSL-0011.
- iFit: sab=iData(‘tsl_0011_D(D2O).zip'); sab=sab(1); % 293 K
S*(a,b) D2O 293K (CAB)

---
ENDF D2O S(q,w)
D2O: S(Q,w) from S(a,b)
GROMACS MD
TIP4P/2005f
coherent
iFit: sqw = Sqw(sab);
CAB model is fair.

---
ENDF Be metal
- ENDF Be does not contain any structure. Fully incoherent, but this is in fact a pure coherent scatterer.
- Some vibrational bands, but there should be phonons…
- iFit:
S(Q,w) 293 K from S(a,b) CAB
iFit:
Be=iData(‘tsl_0026_Bemetal.zip');
Be=Be(9); % 293 K
Sqw = Sqw(iData_Sab(Be));

---
Using all this in iFit
- Load a data set: blah = iData(file);
- Make it a vDOS or Sab or Sqw2D
  - iData_vDOS(..) iData_Sab(…) iData_Sqw2D(…)
- Compute:
  - vdos=dos(sqw2d); sqw2d=incoherent(vdos);
  - sq=structure_factor(sqw2d)
  - sqw2d=coherent(sqw2d, sq);
- Convert
  - Sqw(sab); Sab(sqw2d);

---
Conclusion
- There are models to get S(q,w) from not much.
- Used extensively in ENDF.
- Make up your mind about validity.
- My advices:
  - use it to estimate incoherent when you have a total scattering experiment. Cheaper than polarised beam...
  - ENDF: Extend material descriptions with coherent (structure).